Industrial Grade Nitrile Gloves

Powder Free | Latex Free | 4ml | 100 pcs/box | 10 boxes/carton | S-L

Available Thursday, September 17th

No.GHB2020XG00318

Report Security Code：X048V4

TEST	REPORT

Sample：	Vinyl Nitrile Blend Gloves

Tested Parts：

SHIJIAZHUAGN WALLY PLASTIC CO.,LTD

Classification：

Commissioned test

China National Centre for Quality Supervision and Test of Environmental Protection Products

国家环保产品质量监督检验中心

|  | Test Report |  |  |  |
| --- | --- | --- | --- | --- |
| No.GHB2020XG00318 |  |  | 2 Page Page1 |
|  |  | Specification model |  | L |
| Sample | Vinyl Nitrile Blend Gloves |  |  |  |
|  |  | Brand |  | Wally |
| Client | SHIJIAZHUAGN WALLY PLASTIC | Client |  | Xiaoyun Zhao |
|  | CO.,LTD |  |  |  |
| Tested Part | SHIJIAZHUAGN WALLY PLASTIC | Classification |  | Principal test |
|  | CO.,LTD |  |  |  |
| Nominal Manufacturers | SHIJIAZHUAGN WALLY PLASTIC | Date of manufacture |  | 20200619 |
|  | CO.,LTD |  |  |  |
| Grade | Qualified product | Sample Description |  | Blue |
| Sample Quantity | 30 | Sample Date of arrival |  | 2020-6-23 |
| Judgment Basis | GB 4806.7-2016 |  |  |  |
| Test Standard | GB 4806.7-2016 |  |  |  |
| Test Item | Full items |  |  |  |
|  | The inspected items of the sample meet the requirement of GB 4806.7-2016《National |
|  | Food Safety Standard Food Contact Plastic Materials and Products》. |
| Test |  |  |  |  |
| Conclusion |  | (special seal for inspection) |
|  |  | Date of issue：July 8th in 2020 |
|  | 1、Customers specified simulants and test conditions：10% ethnol、4% |
| Note | acetic acid，70℃，2h； |  |  |  |
|  | 2、The results only apply to samples provided by customer. |  |  |

Approver:	JinpengLiu	Verifier:	Yankun Bai	Producer:	Mengmeng Yang

国家环保产品质量监督检验中心

|  |  | Test | Report（ Appendix） |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| No.GHB2020XG00318 |  |  | 2 Page page2 |  |
| Number |  | Test Items | Unit | Technical |  | Inspection result | Single |
|  |  |  |  | Requirements |  |  | Judgement |
|  |  | Sensory | ------ | Normal color, no odor, |  | Meet the | Pass |
|  |  |  |  | dirt and so on |  | requirements |  |
| 1 | Sensory |  |  |  |  |  |  |
|  | Require |  |  |  |  |  |  |
|  |  | Soak Solution | ------ | The soak obtained from |  |  |  |
|  | -ments |  |  |  |  |  |  |
|  |  |  |  | migration test has no |  | Meet the |  |
|  |  |  |  |  |  |  | Pass |
|  |  |  |  | deterioratioch as turbidity |  | requirements |  |
|  |  |  |  | and precipatation |  |  |  |
|  |  |  |  | abnormal odor |  |  |  |
|  |  | Overall Migration | mg/dm² | ≤10 |  | 2.3 | Pass |
|  |  | （10% ethnol，70 |  |  |  |  |  |
|  |  | ℃，2h） |  |  |  |  |  |
|  |  | Overall migration | mg/dm² | ≤10 |  | 2.2 | Pass |
|  |  | （4%acetic acid，70 |  |  |  |  |  |
|  |  | ℃，2h） |  |  |  |  |  |
|  |  | Potassium permanganate | mg/kg | ≤10 |  | 1.9 | Pass |
|  |  | consumption（water，60 |  |  |  |  |  |
|  |  | ℃，2h） |  |  |  |  |  |
|  | Physic |  |  |  |  |  |  |
| 2 |  | Heavy metals（As Pb） |  |  |  |  |  |
|  | ochemical |  | mg/kg |  |  |  | Pass |
|  |  | [4% acetic acid |  | ≤1 |  | ＜1 |  |
|  | index |  |  |  |  |  |  |
|  |  | （volume fraction ）， |  |  |  |  |  |
|  |  | 60℃，2h] |  |  |  |  |  |
|  |  | Decolorizing test | ------ | Nagative |  | Nagative | Pass |
|  |  | （Vegetable oil |  |  |  |  |  |
|  |  | waping） |  |  |  |  |  |
|  |  | Decolorizing test | ------ | Nagative |  | Nagative | Pass |
|  |  | （Vegetable oil |  |  |  |  |  |
|  |  | waping） |  |  |  |  |  |
|  |  | Decolorizing test | ------ | Nagative |  | Nagative | Pass |
|  |  | （10% ethanol soak， |  |  |  |  |  |
|  |  | 70℃，2h） |  |  |  |  |  |
|  |  | Decolorizing test | ------ | Nagative |  | Nagative | Pass |
|  |  | （4% acetic acid |  |  |  |  |  |
|  |  | soak，70℃，2h） |  |  |  |  |  |
| 3 | Content of vinyl chloride | mg/kg | ≤1 |  | No inspected | Pass |
|  |  |  |  |  | （detection |  |
|  |  |  |  |  |  | limit： 0.1mg/ |  |
|  |  |  |  |  |  | kg） |  |

国家环保产品质量监督检验中心

| 4 | Content of 1,1-dichloroethane | mg/kg | ≤5 | No inspected | Pass |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | （detection |  |
|  |  |  |  | limit： 0.4mg/ |  |
|  |  |  |  | kg） |  |